Technical Data Sheet DR-13-898

DESCRIPTION:

Design Release Coating DR-13-898is a two part UV curable release coating to be used in conjunction with catalyst DC-233 for applications involving roller coater and flexo and gravure presses.

RECOMMENDED USES:

Release coating DR-13-898 for pressure sensitive adhesives where a coating with easy release and high cure speed is required.

PHSICAL DATA:

Appearance: Light amber milky liquid.

Weight/Gallon: 8.9 to 9.1 lbs

Viscosity @770F 600cp to 900 cp

20rpm sp#4

Solids: 100%

Cure (Air Atmosphere):

Design Release Coating DR-13-898 can be cured to tack free coating in an oxygen atmosphere. Actual cure speed depends on coating thickness, and UV energy available for curing.Cure speed can increased with extra catalyst.

STORAGE:

Store at room temperature away from sunlight. Do not store in clear containers. Shell life is six months under recommended conditions.

DISCLAIMER: The information contained herein is based on data considered accurate. However, no warranty is expressed or implied regarding the accuracy of these data results to be obtained from the use thereof. We assume no responsibility for any loss, damage or expense direct or implied arising from the use of this material