Solvent Based Release Coating DR-212

DESCRIPTION:

DR-212 is a solvent based release agent is specifically designed to provide release for polyurethane molding applications. Since DR-212 does not contain any silicone, it is particularly suitable for applications requiring post decoration and adhesion to pressure sensitive adhesive.

APPLICATION:

Mix the coating well before use as waxes and other additives present have a tendency to settle down. A continuous film is required for proper performance.

Excessive application may result in frosted surface. In a situation like this, post application of paint and adhesive could be a problem. Optimize the amount of release agent to prevent excessive application. Multiple release is possible from a single application. DR -212 can be applied by spray, brush, wipe or roll.

PHYSICAL PROPERTIES:

Appearance: White turbid liquid

Specific gravity 0.78(water = 1)

Solids: 10.0 ± 1.0%

Flash Point 1750 F

Storage Stability: Six months